appendix a

Schedule of required data

A1	Schedule of general and technical data

| Ref No | Data to be supplied |
| --- | --- |
| General details |  |
|  | Manufacturer name: |
|  | Type designation: |
|  | Manufacturing period: |
|  | Month/year production commenced: |
|  | Drawings (number/revision): |
| Technical details – conductor |  |
|  | Code name: |
|  | Nominal aluminium equivalent area (mm2): |
|  | Actual cross-sectional area of aluminium (mm2): |
|  | Aluminium alloy (mm2): |
|  | Steel (mm2): |
|  | Optical sub-unit (mm2): |
|  | Total (mm2): |
|  | Number of wires in each layer: (Layer 1 = ) (Layer 2 = ) (Layer 3 = ) |
|  | Diameter and tolerance of wire (mm): |
|  | Lay ratio: |
|  | Overall diameter (mm): |
|  | Rated tensile strength or nominal breaking load (kN): |
|  | Mass per unit length, bare (kg/km): |
|  | Mass per unit length, greased (kg/km): |
|  | Maximum DC resistance at 20°C: |
|  | Coefficient of linear expansion (per 106 °C): |
|  | Stress-strain relationship to BS EN 50182: |
|  | Final modulus of elasticity: |
|  | Short circuit current rating I2t [(kA)2 s]: |
|  | Minimum bend radii (mm): |
| Technical details – grease |  |
|  | Grease type (designation): |
|  | Grease manufacturer: |
|  | Mass per unit length (kg/km): |
|  | Dropping point (°C): |
|  | Oil separation at specified temperature and duration (%): |
| Technical details – individual wires – aluminium/aluminium alloy (Measurement methods as BS EN 50183 and BS EN 60889; measurements to be made after stranding) |  |
|  | Resistivity of aluminium at 20°C (n.m): |
|  | Resistivity of aluminium alloy at 20°C (n.m): |
|  | Minimum tensile strength, aluminium wire (N/mm2) |
|  | Minimum tensile strength, aluminium alloy wire (N/mm2) |
|  | Minimum elongation at failure, aluminium alloy wire (%) |
| Technical details – individual wires – steel or Al clad steel (Measurement methods as BS EN 50189 and BS EN 61232; measurements to be made after stranding) |  |
|  | Number of wires: |
|  | Diameter and tolerance (mm): |
|  | Minimum load at 1% extension for steel wire (N): |
|  | Minimum tensile strength of steel wire (N/mm2): |
|  | % elongation at failure (%): |
|  | Torsional ductility (number of turns to failure): |
|  | Minimum mass of zinc on galvanized steel wire (g/mm2): |
|  | Minimum aluminium thickness of ACS wire (mm): |

A2	Schedule of type test data

| General details |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Product description: |  |  |  |  |  |  |
| Product type: |  |  |  |  |  |  |
| Test data |  |  |  |  |  |  |
| Test Item | Test Ref | Test Report No | Test Date | Compliance (yes, no, n/a) |  |  |
|  |  |  |  | Item | Procedure | Witness |
| Conductor |  |  |  |  |  |  |
| Surface condition | BS EN 50182 |  |  |  |  |  |
| Diameter | BS EN 50182 |  |  |  |  |  |
| Inertness | BS EN 50182 |  |  |  |  |  |
| Lay ratio and direction of lay | BS EN 50182 |  |  |  |  |  |
| Number and type of wires | BS EN 50182 |  |  |  |  |  |
| Mass per unit length | BS EN 50182 |  |  |  |  |  |
| Stress-strain curve | BS EN 50182 |  |  |  |  |  |
| Tensile breaking strength | BS EN 50182 |  |  |  |  |  |
| Stringing test (if applicable) | BS EN 50182 |  |  |  |  |  |
| Grease mass per unit length | BS EN 50182 |  |  |  |  |  |
| Stability of grease in conductor | BS EN 50182 |  |  |  |  |  |
| Fatigue life | ES400C25 & IEC 60794 |  |  |  |  |  |
| Fault current I2t measurement | ES400C25 & IEC 60794 |  |  |  |  |  |
| Lightning simulation | ES400C25 & IEC 60794 |  |  |  |  |  |
| Running blocks | ES400C25 |  |  |  |  |  |
| Temperature cycle | ES400C25 & IEC 60794 |  |  |  |  |  |
| Aluminium wires to BS EN 60889 or Aluminium Alloy wires to BS EN 50183 |  |  |  |  |  |  |
| Visual | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Diameter | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Tensile strength | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Elongation | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Resistivity | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Wrapping | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Welding | BS EN 60889 BS EN 50183 |  |  |  |  |  |
| Zinc coated steel wires to BS EN 50189 |  |  |  |  |  |  |
| Visual | BS EN 50189 |  |  |  |  |  |
| Diameter | BS EN 50189 |  |  |  |  |  |
| Tensile strength | BS EN 50189 |  |  |  |  |  |
| Stress at 1% extension | BS EN 50189 |  |  |  |  |  |
| Torsion test | BS EN 50189 |  |  |  |  |  |
| Wrapping test | BS EN 50189 |  |  |  |  |  |
| Mass of zinc coating | BS EN 50189 |  |  |  |  |  |
| Zinc dip test | BS EN 50189 |  |  |  |  |  |
| Adhesion of zinc coating | BS EN 50189 |  |  |  |  |  |
| Aluminium clad steel wires to BS EN 61232 |  |  |  |  |  |  |
| Visual | BS EN 61232 |  |  |  |  |  |
| Finish | BS EN 61232 |  |  |  |  |  |
| Diameter | BS EN 61232 |  |  |  |  |  |
| Tensile stress | BS EN 61232 |  |  |  |  |  |
| Elongation | BS EN 61232 |  |  |  |  |  |
| Torsion | BS EN 61232 |  |  |  |  |  |
| Resistivity | BS EN 61232 |  |  |  |  |  |
| Minimum aluminium thickness | BS EN 61232 |  |  |  |  |  |
| Stress at 1% extension | BS EN 61232 |  |  |  |  |  |
| Grease |  |  |  |  |  |  |
| High temperature stability test | BS EN 50326 |  |  |  |  |  |
| Penetrability test | BS EN 50326 |  |  |  |  |  |
| Adhesion test | BS EN 50326 |  |  |  |  |  |
| Ageing test | BS EN 50326 |  |  |  |  |  |
| Corrosion test | BS EN 50326 |  |  |  |  |  |
| Stability in complete conductor | BS EN 50326 |  |  |  |  |  |
| Fibres |  |  |  |  |  |  |
| Tensile performance | IEC 60794 |  |  |  |  |  |
| Temperature cycling | IEC 60794 |  |  |  |  |  |
| Water penetration | IEC 60794 |  |  |  |  |  |
| Bleeding of tube compound | IEC 60794 |  |  |  |  |  |